Figure S1. Concentration of nTiO2 suspended in water over a 96-h time period. Initial concentration was 2.5 mg TiO2/L (P25, Evonik Aeroxide®). Measured as 49Ti (mean ± standard deviation; n=5) in ASTM (American Society of Testing and Materials) reconstituted hard fresh water (192 mg/L NaHCO3, 120 mg/L CaSO4·2H2O, 120 mg/L MgSO4, 8 mg/L KCl).